**Qualification Results Summary of 10x10, 12x12 TQFP\_EP Using G700L/8361J at Amkor Philippines**

|  |
| --- |
| QUALIFICATION PLAN / STATUS |
| **Test** | **Specification** | **Sample Size** | **Results** |
| Temperature Cycle (TC)\* | JEDEC*JESD22-A104* | 3 x 32 | Pass |
| Unbiased HAST (uHAST)\* | JEDEC *JESD22-A118* | 3 x 32 | Pass |
| Highly Accelerated Stress Test (HAST)\* | JEDEC *JESD22-A110* | 3 x 32 | Pass |
| Solder Heat Resistance(SHR)\* | JEDEC/IPC *J-STD-020* | 3 x 11 | Pass |
| High Temperature Storage Life(HTSL) | JEDEC *JESD22-A103* | 1 x 32 | Pass |
| Electrostatic Discharge*Field-Induced Charged**Device Model* | JEDEC *JESD22-C101* | 3/voltage | Pass 1250 V |

\*Preconditioned per JEDEC/IPC J-STD-020