**Qualification Results Summary of Revision to Thickness of Polyimide and Redistribution Layers for ADN8833 and ADN8834 in WLCSP**

|  |
| --- |
| QUALIFICATION PLAN |
| **Test** | **Specification** | **Sample Size****(lot\*sample)** | **Results** |
| Temperature Cycle (TC)-40C to +125C (1 cycle/hour)500 cycles | JEDEC*JESD22-A104* | **3\*77** | **Pass** |
| Unbiased HAST (UHAST)130C / 85% RH96 hours | JEDEC *JESD22-A118* | **3\*25** | **Pass** |
| Electrostatic Discharge*Field-Induced Charged Device Model* | JEDEC*JS-002* | **1\*18****3/voltage** | **Pass** |