**Qualification Results Summary of Revision to Thickness of Polyimide and Redistribution Layers for ADN8833 and ADN8834 in WLCSP**

|  |  |  |  |
| --- | --- | --- | --- |
| QUALIFICATION PLAN | | | |
| **Test** | **Specification** | **Sample Size**  **(lot\*sample)** | **Results** |
| Temperature Cycle (TC)  -40C to +125C (1 cycle/hour)  500 cycles | JEDEC*JESD22-A104* | **3\*77** | **Pass** |
| Unbiased HAST (UHAST)  130C / 85% RH  96 hours | JEDEC *JESD22-A118* | **3\*25** | **Pass** |
| Electrostatic Discharge  *Field-Induced Charged Device Model* | JEDEC*JS-002* | **1\*18**  **3/voltage** | **Pass** |