**LTC3548A - Silicon Changes to Improve Latch Immunity**

A comparison of the latch up performance between the old silicon and the new silicon shows that the new silicon is much better, see the table below:

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| Silicon | CH1: SW Above Vin (SW-Vin), V  Latch Up Voltage | CH1: SW below GND (SW-GND), V  Latch Up Voltage | CH2: SW Above Vin (SW-Vin), V  Latch Up Voltage | CH2: SW below GND (SW-GND), V  Latch Up Voltage |
| Old | 3.3 | -2.5 | 2.8 | -2.9 |
| New | No Latch Up out to 4.5V | No Latch Up out to -5V | No Latch Up out to 4.5V | No Latch Up out to -5V |