Summary of Supporting Information:

JCET 8L SOIC AD8051/AD8091 (XFCB):

| Test Name | Specification | Conditions | Device | Package | Lot # | Sample Size | Qty. Failures |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Autoclave (AC)1 | JESD22-A102 | 121°C 100%RH 2atm 96 hours | AD8091 | JCET 8-SOIC_N | Q7515.2 | 77 | 0 |
|  |  |  |  |  | Q7515.16 | 77 | 0 |
|  |  |  |  |  | Q7515.33 | 77 | 0 |
| Biased HAST (HAST)2 | JESD22-A110 | 130°C 85%RH 2atm, Biased 96 hours | AD8091 | JCET 8-SOIC_N | Q7515.17 | 77 | 0 |
|  |  |  |  |  | Q7515.19 | 77 | 0 |
|  |  |  |  |  | Q7515.36 | 77 | 0 |
| High Temperature Storage Life (HTSL) | JESD22-A103 | 150°C 1,000 hours | AD8091 | JCET 8-SOIC_N | Q7515.26 | 77 | 0 |
| Solder Heat Resistance (SHR)1 | ADI-0049 |  | AD8091 | JCET 8-SOIC_N | Q7515.24 | 16 | 0 |
|  |  |  |  |  | Q7515.25 | 16 | 0 |
|  |  |  |  |  | Q7515.42 | 16 | 0 |
| Temperature Cycling (TC)1 | JESD22-A104 | -65°C / +150°C 500 cycles | AD8091 | JCET 8-SOIC_N | Q7515.8 | 77 | 0 |
|  |  |  |  |  | Q7515.21 | 77 | 0 |
|  |  |  |  |  | Q7515.22 | 77 | 0 |

JCET 8L SOIC OP282 (Large Die)

| Test Name | Specification | Conditions | Package | Device | Lot # | Sample Size | Qty. Failures |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Autoclave (AC)1 | JESD22-A102 | 121°C 100%RH 2atm 96 hours | JCET 8-SOIC_N | OP282 | Q7835.100 | 77 | 0 |
|  |  |  |  |  | Q7835.101 | 77 | 0 |
|  |  |  |  |  | Q7835.102 | 77 | 0 |
| Biased HAST (HAST)1 | JESD22-A110 | 130°C 85%RH 2atm, Biased 96 hours | JCET 8-SOIC_N | OP282 | Q7835.200 | 77 | 0 |
|  |  |  |  |  | Q7835.201 | 77 | 0 |
|  |  |  |  |  | Q7835.202 | 77 | 0 |
| High Temperature Storage Life (HTSL) | JESD22-A103 | 150°C 1,000 hours | JCET 8-SOIC_N | OP282 | Q7835.300 | 77 | 0 |
| Solder Heat Resistance (SHR)1 | ADI-0049 |  | JCET 8-SOIC_N | OP282 | Q7835.400 | 21 | 0 |
|  |  |  |  |  | Q7835.401 | 21 | 0 |
|  |  |  |  |  | Q7835.402 | 21 | 0 |
| Temperature Cycling (TC)1 | JESD22-A104 | -65°C / +150°C 500 cycles | JCET 8-SOIC_N | OP282 | Q7835.500 | 77 | 0 |
|  |  |  |  |  | Q7835.501 | 77 | 0 |
|  |  |  |  |  | Q7835.502 | 77 | 0 |