| Package | Assembly Site | Autoclave1 121°C, 100%RH, 2 atm, 96 hrs | HAST1,2 130C 85%RH 2atm, Biased | HTS1,2 150°C, 1000 hrs | SHR (Solder Heat Resistance) | Temp Cycle1,2 -65°C to 150°C, 500 cycles |
| --- | --- | --- | --- | --- | --- | --- |
| MINI_SOIC | Carsem | Pass | Pass | Pass | Pass | Pass |
|  | TOTAL: | 0 fails/231 samples | 0 fails/231 samples | 0 fails/77 samples | 0 fails/33 samples | 0 fails/231 samples |

AEC-Q100 QUALIFICATION RESULTS: PCN 10_0006 Rev C

1 Parts subjected to preconditioning per J-STD-0020, MSL 1 with peak reflow temperature of 260°C prior to stress

2Parts were electrically tested at ambient and hot temperatures.