QUALIFICATION RESULTS: PCN 10_0008

| Package | Assembly Site | Autoclave1 | HAST/THB1 | HTS | Temp Cycle1 |
| --- | --- | --- | --- | --- | --- |
|  |  | 121°C, 100%RH, 2 atm, 96 hrs | 130°C, 85%RH, 2 atm, Biased, 96 hrs | 150°C, 1000 hrs | -65°C to 150°C, 500 cycles |
| SC70 | Carsem | Pass | Pass | Pass | Pass |
|  | TOTAL: | 0 fails/492 samples | 0 fails/246 samples | 0 fails/164 samples | 0 fails/566 samples |

1 Parts subjected to preconditioning per J-STD-0020, MSL 1 with peak reflow temperature of 260°C prior to stress