PCN 12_0130

| Test | Conditions | Sample Size | Results |
| --- | --- | --- | --- |
| Autoclave (AC) | JEDEC JESD22-A102 | 3 x 45 | Pass |
| Highly Accelerated Stress Test (HAST) | JEDEC JESD22-A110 | 3 x 45 | Pass |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 1 x 45 | Pass |
| Low Temperature Storage (LTS) | JEDEC JESD22-A119 | 1 x 45 | Pass |
| Random Drop | CAM0091 | 3 x 45 | Pass |
| Solder Heat Resistance (SHR) | ADI-0049 | 3 x 11 | Pass |
| Temperature Cycle (TC) | JEDEC JESD22-A104 | 3 x 45 | Pass |
| Temperature Humidity Bias (THB) | JESD22-A101 | 3 x 45 | Pass |