**PCN 13\_0070  
Qualification Summary**



|  |  |  |  |
| --- | --- | --- | --- |
| **Test** | **Conditions** | **Sample Size** | **Result** |
| Temperature Cycle\* | JESD22, Method A104  Condition G  -40°C to +125°C.  1000 cycles  Data points at 200, 500 and 1000 cycles. | 32 | Pass |
| High Temperature Operating Life\* | JESD22, Method A108  125°C TA/TC  500 Hr. | 16 | Pass |
| Unbiased HAST | JESD22, Method A110  130°C / 85% RH 2atm  Unbiased 96Hr. | 16 | Pass |

\*Preconditioned Per JEDEC/IPC J-STD-020 prior to this stress test.