Qual Summary

| QUALIFICATION SUMMARY/RESULTS |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 3 x 77 | Pass |
| Temperature Cycle (TC)* | JEDEC JESD22-A104 | 9 x 77 | Pass |
| Autoclave (AC)* | JEDEC JESD22-A102 | 6 x 77 1 x 45 | Pass |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 1 x 77 1 x 45 | Pass |
| Latch-Up | JEDEC Standard 78 | 1x6 | Pass |
| Electrostatic Discharge Human Body Model | ESDA/JEDEC JS-001-2011 | 1x24 | Pass ±3500V |
| Electrostatic Discharge Field-Induced Charged Device Model | JESD22-C101 | 1x18 | Pass ±1000V |
| Electrostatic Discharge Machine Model | JESD22-A115 | 1x18 | Pass ±100V |

*Preconditioned per JEDEC/IPC J-STD-020